CutSpecTM for Concrete Treatments system:

Product: Dryshield

For comprehensive manufacturer instructions, visit https://greenumbrellasystems.com/dryshield-concrete-treatment/

EarlyAge Conventional Concrete (28 days or earlier):

DryShieldTM by Green Umbrella® of Rochester, NY (844) 200-7336 is a R.T.U. (Ready to Use), S.O.L.O. (Spray-On, Leave-On), Penetrating Completely Reactive Insoluble Nano Densifier silica solution to strengthen, seal and densify the concrete surface. Clean and sweep all debris and potential contaminants—including sealers, wax, coatings, and oil or food spills—before processing. Place on @EarlyAgeTM concrete, the same day of concrete placement and finishing; once the concrete is hard enough for walking or as specified in the construction process. DryShieldTM is NOT a cure & seal. Apply DryShieldTM in temperatures 40 (and rising) -95°F (4-35°C) at 400-500 SF per gallon. Keep wet for a dwell time of 30 minutes. Allow to air dry. (For certified installers and manufacturer instructions visit www.GreenUmbrellaSystems.com)

EarlyAge Concrete to Be Abrasively Trowel Polished (PHP):

DryShieldTM by Green Umbrella® of Rochester, NY (844) 200-7336 is a R.T.U. (Ready to Use), S.O.L.O. (Spray-On, Leave-On), Penetrating Completely Reactive Insoluble Nano Densifier silica solution to strengthen, seal and densify the concrete surface. Clean and sweep all debris and potential contaminants—including sealers, wax, coatings, and oil or food spills—before processing. For an abrasively trowel polished, processed using a power trowel machine adapted for concrete polishing. Place on @EarlyAgeTM concrete a few days after concrete place- ment and finishing or as specified in the construction process by Green Umbrella. Use an Integrally Troweled Concrete Placement (ITCP) process 1) During concrete placement & after finishing, use Green Umbrella IceStartTM cure and IceStop concrete cure system 2) Wet profile and hone with GCTM abrasives with GreenCutTM cutting agent. 3) Optional: Apply Green Umbrella NanoDyeTM for colorant 4) Apply DryShieldTM in temperatures 40 (and rising) -95°F (4-35°C) at 400-500 SF per gallon. Keep wet for a dwell time of 30 minutes. Allow to air dry. 5) Hone and polish to desired finish with GCTM abrasives. 6) Apply Green Umbrella MicrofilmTM - a penetrat- ing, reactive, interior micro-finish for profiled surfaces - at a rate of 1000-1200 SF per gallon. 7) Burnish with GreenGlossTM concrete-weighted, high-speed burnisher GreenGlossTM pads. (For certified installers and manu- facturer instructions, visit www.GreenUmbrellaSystems.com)

MatureAge Conventional Concrete (28 days or later):

DryShieldTM by Green Umbrella® of Rochester, NY (844) 200-7336 is a R.T.U. (Ready to Use), S.O.L.O. (Spray-On, Leave-On), Penetrating Completely Reactive Insoluble Nano Densifier silica solution to strengthen, seal and densify the concrete surface. Clean and sweep all debris and potential contaminants—including sealers, wax, coatings, and oil or food spills—before processing. At 28 days or later place on @MatureAgeTM concrete or as speci- fied in the construction process. Apply DryShieldTM in temperatures 40 (and rising) -95°F (4-35°C) at 400-500 SF per gallon. Keep wet for a dwell time of 30 minutes. Allow to air dry. (For certified installers and manufacturer instructions visit www.GreenUmbrellaSys- tems.com)

MatureAge Conventional Concrete To Be Abrasively Polished (PHP):

DryShieldTM by Green Umbrella® of Rochester, NY (844) 200-7336 is a R.T.U. (Ready to Use), S.O.L.O. (Spray-On, Leave-On), Penetrating Completely Reactive Insoluble Nano Densifier silica solution to strengthen, seal and densify the concrete surface. Clean and sweep all debris and potential contaminants—including sealers, wax, coatings, and oil or food spills—before processing. For a profiled, honed, and polished (PHP) concrete floor processed using a variable abrasive, planetary grinding machine to remove existing coatings, surface imperfec- tions, and flattening the concrete slab. Place on @MatureAgeTM concrete as specified in the construction process by Green Umbrella. 1) Wet profile and hone with GCTM abrasives with GreenCutTM cutting agent. 2) Optional: Apply Green Umbrella NanoDyeTM for colorant 3) Apply DryShieldTM in temperatures 40 (and rising) -95°F (4-35°C) at 400-500 SF per gallon. Keep wet for a dwell time of 30 minutes. Allow to air dry. 4) Hone and polish to desired finish with GCTM abrasives. 5) Apply Green Umbrella MicrofilmTM - a penetrating, reactive, inte- rior micro-finish for profiled surfaces - at a rate of 1000-1200 SF per gallon. 6) Burnish with GreenGlossTM con- crete-weighted, high-speed burnisher GreenGlossTM pads. (For certified installers and manufacturer instruc- tions, visit www.GreenUmbrellaSystems.com)

For full CSI specifications: https://greenumbrellasystems.com/specifications/

Contact Technical Sales: info@greenumbrellasystems.com

Green Umbrella 5/2020

1-800