CutSpecTM for Concrete Sealer

Product: Interior Microfilm

For comprehensive manufacturer instructions, visit https://greenumbrellasystems.com/interior-microfilm/

@EarlyAge Conventional Concrete (28 Days Or Earlier):
For sealers better suited to @EarlyAge concrete that is hard trowel or broom finished see Green Umbrella IceCapTM, Exterior MicroFilmTM or ColorShieldTM. (For certified installers and manufacturer instructions visit www.GreenUmbrellaSystems.com)

@EarlyAge Concrete To Be Abrasively Trowel Polished (PHP):
Interior MicroFilmTM by Green Umbrella® of Rochester, NY (844) 200-7336 is a R.T.U. (Ready to Use), S.O.L.O. (Spray-On, Leave-On), Sub-Surface Penetrating, Completely Reactive, Contaminant Resistant, Insoluble, Nano-Protectant solution to strengthen, seal, and protect the concrete surface and subsurface. Clean and sweep all debris and potential contaminants—including sealers, wax, coatings, and oil or food spills—before application. For a profiled, honed, and polished (PHP) concrete floor @EarlyAge - place and finish using GreenIceTM integral trowel cure. Place on @EarlyAgeTM concrete as specified in the construction process by Green Umbrella. As soon as 72 hours after placement, process using a variable speed, planetary grinding machine (propane power preferred) to remove existing coatings, surface imperfections, profiling and flattening the concrete slab. 1) Wet profile with GCTM abrasives and GreenCutTM liquid cutting agent. 2) Wet hone with GCFusionTM or GCErasersTM to produce necessary surface profile. 3) Optional for MaxDefense with Color: Apply Green Umbrella Nano-DyeTM as colorant 4) Apply DryShieldTM in temperatures 40°F (4°C) [and rising] up to 95°F (35°C) at 400-800 SF per gallon. Keep wet for a dwell time of 30 minutes. Allow to air dry. 5) Auto scrub using soft bristle brushes, green or red pads to remove any excess material or potential contaminants. 6) Apply Shield & EnhanceTM in temperatures 40°F (4°C) [and rising] up to 95°F (35°C) at 400-800 SF per gallon. Keep wet for a dwell time of 30 minutes. Allow to air dry. 7) Polish to desired finish with GCPolish-Plus TM abrasives. 8) Auto scrub using soft bristle brushes, green or red pads and a recommended Green Umbrella cleaning treatment to remove all potential contaminants. 9) Apply Green Umbrella Interior MicroFilmTM - a penetrating, reactive, interior, micro-finish for profiled surfaces - at a rate of 1500-2500 SF per gallon, first coat. Allow to air dry. 10) Apply a second coat. Allow to air dry. 11) Burnish with GreenGlossTM concrete-weighted, high-speed burnisher equipped with GreenGlossTM pads. 12) For MaxDefense - return 48 hours+ after second coat, clean and apply a THIRD coat of Interior MicroFilmTM. Allow to air dry. Burnish. For certified installers and manufacturer instructions, visit www.GreenUmbrellaSystems.com

@MatureAge Conventional Concrete (28 days or earlier):
For sealers better suited to @MatureAge concrete that is hard trowel or broom finished see Green Umbrella IceCapTM, Exterior MicroFilm TM or ColorShieldTM. (For certified installers and manufacturer instructions visit www.GreenUmbrellaSystems.com)

@MatureAge Conventional Concrete To Be Abrasively Polished:
Interior MicroFilmTM by Green Umbrella® of Rochester, NY (844) 200-7336 is a R.T.U. (Ready to Use), S.O.L.O. (Spray-On, Leave-On), Sub-Surface Penetrating, Completely Reactive, Contaminant Resistant, Insoluble,
Nano-Protectant solution to strengthen, seal, and protect the concrete surface and subsurface. Clean and sweep
all debris and potential contaminants—including sealers, wax, coatings, and oil or food spills—before applica-
tion. For a profiled, honed, and polished (PHP) concrete floor place on @MatureAgeTM concrete as specified in
the construction process by Green Umbrella. Process using a variable speed, planetary grinding machine
(propane power preferred) to remove existing coatings, surface imperfections, profiling and flattening the
concrete slab. 1) Wet profile with GCTM abrasives and GreenCutTM liquid cutting agent. 2) Wet hone with GCFu-
sionTM or GCErasersTM to produce necessary surface profile. 3) Optional for MaxDefense with Color: Apply Green
Umbrella Nano-DyeTM as colorant 4) Apply DryShieldTM in temperatures 40°F (4°C) [and rising] up to 95°F (35°C)
at 400-800 SF per gallon. Keep wet for a dwell time of 30 minutes. Allow to air dry. 5) Auto scrub using soft bristlebrushes, green or red pads to remove any excess material or potential contaminants. 6) Apply Shield & EnhanceTM in temperatures 40°F (4°C) [and rising] up to 95°F (35°C) at 400-800 SF per gallon. Keep wet for a dwell time of 30 minutes. Allow to air dry. 7) Polish to desired finish with GCPolishPlusTM abrasives. 8) Auto scrub using soft bristle brushes, green or red pads and a recom- mended Green Umbrella cleaning treatment to remove all potential contaminants. 9) Apply Green Umbrella Interior MicroFilmTM - a pene- trating, reactive, interior, micro-finish for profiled surfaces - at a rate of 1500-2500 SF per gallon, first coat. Allow to air dry. 10) Apply a second coat. Allow to air dry. 11) Burnish with GreenGlossTM concrete-weighted, high-speed burnisher equipped with GreenGlossTM pads. 12) For MaxDefense - return 48 hours+ after second coat, clean and apply a THIRD coat of Interior MicroFilmTM. Allow to air dry. Burnish. For certified installers and manufacturer instructions, visit www.GreenUmbrellaSystems.com

For full CSI specifications: https://greenumbrellasystems.com/specifications/

Contact Technical Sales: info@greenumbrellasystems.com

Green Umbrella 5/2020

1-800