SECTION 033509 – CONCRETE CURE AND FINISHING SYSTEMS

This Specification is provided only as a guide and is intended to be used as a guideline for the preparation and installation of Green Umbrella products as systems. This Specification follows CSI MasterFormat™ and can be used to specify Green Umbrella products, but it should be edited and tailored to the needs of each specific project.

General sustainability requirements have been considered in the preparation of this Specification, but due to individual project goals, regional requirements, and other factors, sustainability requirements for each project must be confirmed and verified, then coordinated with the architectural concrete system manufacturer to ensure selection of the most appropriate products.

- GENERAL

      - SUMMARY

        - Section Includes:

Specifier Note: Coordinate concrete finishing and curing requirements with Division 03 cast-in-place concrete section.

          - Concrete floor slab Curative / Finish Aid / Fixative / Densifier System as specified.

Specifier Note: Retain the following subparagraph if protecting the concrete during construction is required.

          - Protecting finished concrete floor slab until Substantial Completion.

      - RELATED REQUIREMENTS

        - Concrete, including formwork, reinforcement, concrete materials, mixture design, placement procedures, initial finishing and curing. Additional requirements are specified in Section 033000 "Cast-in-Place Concrete."

          - Coordinate with the following Sections:

Specifier Note: Edit the following list of Sections applicable to the project requirements.

            - Section 032400 - Fibrous Reinforcing.

            - Section 033000 - Cast-in-Place Concrete.

            - Section 033500 - Concrete Finishing.

            - Section 033900 - Concrete Curing.

            - Section 079200 - Joint Sealants.

          - Coordinate with finishing manufacturer for system "products" for sections above.

      - REFERENCES

        - ASTM International (ASTM):

          - ASTM C94/C94M: Standard Specification for Ready-Mixed Concrete

          - ASTM C156: Standard Test Method for Water Loss (from a Mortar Specimen) Through Liquid Membrane–Forming Curing Compounds for Concrete.

          - ASTM C779/C779M: Standard Test Method for Abrasion Resistance of Horizontal Concrete Surfaces.

          - ASTM C805/C805M: Standard Test Method for Rebound Number of Hardened Concrete.

          - ASTM C944/C944M: Standard Test Method for Abrasion Resistance of Concrete or Mortar Surfaces by the Rotating–Cutter Method.

          - ASTM C979/C979M: Standard Specification for Pigments for Integrally Colored Concrete.

          - ASTM C1077: Standard Practice for Agencies Testing Concrete and Concrete Aggregates for Use in Construction and Criteria for Testing Agency Evaluation.

          - ASTM C1116/C1116M: Standard Specification for Fiber-Reinforced Concrete.

          - ASTM C1583/C1583M: Standard Test Method for Tensile Strength of Concrete Surfaces and the Bond Strength or Tensile Strength of Concrete Repair and Overlay Materials by Direct Tension (Pull-off Method).

          - ASTM C1895 - Standard Test Method for Determination of Mohs Scratch Hardness.

          - ASTM E96/E96M–10: Standard Test Method for Water Vapor Transmission of Materials.

          - ASTM E329: Standard Specification for Agencies Engaged in Construction Inspection, Testing, or Special Inspection.

          - ASTM E1155: Standard Test Method for Determining FF Floor Flatness and FL Floor Levelness Numbers.

          - ASTM G152: Standard Practice for Operating Open Flame Carbon Arc Light Apparatus for Exposure of Nonmetallic Materials.

        - American National Standards Institute (ANSI):

          - ANSI/NFSI B101.1-2009: Test Method for Measuring Wet SCOF of Common Hard-Surface Floor Materials.

          - ANSI/NFSI B101.3-2012: Test Method for Measuring Wet DCOF of Common Hard-Surface Floor Materials

        - American Concrete Institute (ACI):

          - ACl 302.1R-89-15: Guide to Concrete Floor and Slab Construction.

          - ACI 305.1-14(20) Specification for Hot Weather Concreting (Reapproved 2020).

          - ACI 306.1-90: Standard Specification for Cold Weather Concreting (Reapproved 2002).

        - British Standard (BS):

          - BS EN 13892-4:2002: Methods of Test for Screed Materials. Determination of Wear Resistance BCA.

        - Concrete Sawing and Drilling Association, Inc. (CSDA):

          - CSDA ST-115: Measuring Concrete Micro Surface Texture.

        - International Code Council Evaluation Service (ICC ES):

          - ICC ES AC 32: Concrete with Synthetic Fibers.

      - PREINSTALLATION MEETING

        - Preinstallation Conference: Conduct conference at project site or video conference.

          - Schedule meeting between 7 and 14 days prior to first concrete slab placement of 10,000 SF or greater and after placement of test slab and after concrete submittals have been approved.

          - Obtain Pre-slab Installation Meeting Agenda from Green Umbrella, (844) 200-7336.

          - Require responsible representatives of each party involved with the interior concrete slab work to attend the meeting. Representatives to be present shall include personnel who are directly involved in overseeing the work for each placement and who have authority to control the concreting work.

          - Before submitting design mixtures, review concrete design mixture and review quality procedures for concrete materials, installation procedures, and compatibility with concrete densification and finish materials.

          - Require representatives of each entity directly concerned with concrete.  Attendees shall include, but not be limited to the following:

            - Owner’s [Construction Manager] [General Contractor].

            - Owner’s Concrete Consultant.

            - Contractor:

              - Project Manager.

              - Superintendent.

            - Green Umbrella Certified Place/Finish Concrete Subcontractor:

              - Green Umbrella Master Craftsman/Project Manager.

              - Green Umbrella Craftsman/Finish Foreman.

            - Concrete Producer:

              - Quality Control Representative.

            - Subcontractor responsible for fine grading and sub-base preparation for concrete slabs on grade.

            - Owner’s Construction Testing Laboratory.

            - Independent testing agency responsible for concrete design mixtures.

          - Review sequencing of cast-in-place concrete requirements as specified herein. Review application, curing procedures, construction joints, concrete repair procedures, concrete finishing and protection of newly placed and finished concrete.

          - Meeting Minutes:  Record on the agenda document, discussions of meeting and decisions and agreements reached.  Submit in accordance with the requirements of Submittals paragraph.

          - Changes to Contract Documents from recommendations or discussions at the Pre-slab Installation Meeting shall be approved in writing by Owner’s [Construction Manager] [General Contractor] prior to implementation.

      - SCHEDULING

Specifier Note: The following time period is optimal for slabs receiving subsequent polishing treatments. Concrete slabs incorporating Green Umbrella GreenIce systems can bear pedestrian traffic within three to five hours after placement and finishing.  However, best concrete practice should allow three to five days before allowing polishing equipment and other construction procedures involving weight-bearing equipment on new concrete slabs.

        - Give preference to Thursday or Friday placement and finishing to reduce interference and expedite project release to other trades.

      - ACTION SUBMITTALS

        - General: Provide submittals as required by this Specification in accordance with Contract Documents. No work shall be performed relating to a submittal until the submittal is approved by the Architect/Engineer in writing.

        - Submit submittal items concurrently for submittals shown with the same submittal date specified in the Concrete Submittal Register included at the end of this Section. Do not submit submittals of this section together with submittals in any other Section. Identify submittals explicitly in accordance with the requirements of Section 013300.

        - Green Umbrella Certified Place/Finish Concrete Subcontractor Qualification Statement: Submit Green Umbrella Certification Form including Floor Finisher Qualifications as required in Quality Assurance paragraph.

      - Provide ACI certification documents for at least three finishers who will install all interior slab placements.

        - Slab Joint and Placement Plan:

          - Develop and submit slab joint and placement plan. Plan shall identify the following:

            - Exterior walls and column grid locations.

            - Truck access location.

            - Extent of pours including width, length, slab placement area and volume.

            - Sequence of placement.

            - Location of test slab placement.

            - Locations of construction joints.

        - Location of sawn contraction joints when locations differ from those shown on the structural drawings.

        - Product Data: Material and Technical Data for all materials including, but not limited to:

          - Concrete: Provide concrete plant record of concrete mix, including additives and on-site water quantity compensation, reviewed by architect and floor system manufacturer.

Specifier Note: Retain subparagraph below if fiber reinforcement is to be added to concrete mix.

          - Fiber reinforcement material.

          - Concrete cure treatment(s).

Specifier Note: Retain Subparagraph below if Repair products are to be used to warranty project.

          - Repair materials.

            - Surface Defect Repairs: The Owner’s Representative shall submit map of locations where surface defects are to be repaired. Map shall be referenced to the building column line locations.

            - Crack Repair: The Owner’s Representative shall submit a map of locations where cracking is to be repaired. Map shall be referenced to the building column line locations.

Specifier Note: Retain subparagraphs below if floor is in the dry and protection is to cover the slab during construction.

          - Interior slab protection materials.

Specifier Note: Retain Subparagraphs below if slab is exposed to wear and protection is to cover the slab during construction.

          - Exterior slab protection materials.

        - System Data: Technical data, testing and surface profile requirements for completed concrete finish system.

        - Concrete Floor Protection Plan: Submit concrete floor protection plan addressing procedures specified in Part 3 of this Section.

        - Shop Drawings: Application area plans to show expansion joints and layout of colorant(s), indication of topical or integral (if specified). Indicate locations and schedule of concrete placement, integral troweled cure and abrasive profile.

        - Sustainable Design Submittals:

Specifier Note: Include test reports and CDPH compliance when seeking low emitting materials credits for sustainable design requirements.

          - Laboratory Test Reports: For liquid concrete treatments, indicating compliance with requirements for low-emitting materials.

          - Products shall comply with the requirements of the California Department of Public Health's (CDPH) "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

        - Pre-Slab Installation Meeting Documents:

          - Record of notification of pre-slab meeting including company name, persons contacted, date, and method of contact.

          - Meeting Agenda

          - Meeting Minutes. Submit meeting minutes including attendance record to participants and Owner’s Construction Manager.  Minutes of the meeting shall be distributed to partied in attendance by the Contractor within 5 days of the meeting.  One copy of the minutes shall also be transmitted to Green Umbrella for informational purposes.

Specifier Note: Coordinate delivery ticket submittal requirements with Section 033000.

        - Delivery Tickets:

          - Submit delivery tickets for each load of concrete delivered to site.

          - Indicate information required by ASTM C 94 on each ticket including additional information required for slabs.

          - Information on ticket shall include quantities of all material batched including the amount of free water in the aggregate and the quantity of water that can be added at the site without exceeding the maximum water cement ratio of the approved mix design. Aggregate moisture corrections shall be based on ASTM definitions of aggregate moisture content and absorption.

          - Mix identification number on ticket shall match number on submitted and approved mix design.

      - INFORMATIONAL SUBMITTALS

        - Product Test Reports: Provide testing reports for each product. Indicate entity performing the testing, testing standards and results and the qualified testing agency that approves or certifies the testing and results.

        - Provide manufacturer’s written installation instructions and recommendations.

Specifier Note: Retain paragraph below if contractor is responsible for field quality control and reporting.

        - Field quality control reports.

        - Testing agency qualifications.

        - Installer qualifications.

      - CLOSEOUT SUBMITTALS

        - Maintenance Data: Manufacturer’s written recommendations for protecting, cleaning, and maintaining concrete finishes.

      - QUALITY ASSURANCE

        - Testing Agency Qualifications: An independent testing agency qualified to perform specified or required testing in accordance with ASTM C1077 and ASTM E329.

        - Placement and Finisher Qualifications: A firm currently certified by Green Umbrella as a Craftsman or Master Craftsman prior to project award. Installer must provide written documentation from the manufacturer confirming the Installer’s current accreditation and training from Green Umbrella on installation of the Green Umbrella GreenIce System and related equipment and processes. Failure to provide current accreditation will void any warranty implied or otherwise associated with the Green Umbrella Architectural Concrete System.

          - Acceptable Green Umbrella Master Craftsman: (www.greenumbrellasystems.com)

            - Contact Info. tom@greenumbrellasystems.com or Ben@greenumbrellasystems.com

        - Manufacturer’s Representative: Provide oversight and inspection by concrete finish manufacturer in accordance with manufacturer’s requirements.

          - Green Umbrella Representative: (www.greenumbrellasystems.com)

            - Contact Info. tom@greenumbrellasystems.com, 716-771-6352, or Ben@greenumbrellasystems.com , 208-910-9178

        - Mockups: Construct mockups [as indicated on Drawings], [as directed by Architect], [minimum 20x20 feet] for each finish to verify selections made and to demonstrate typical joints, surface profile and gloss, tolerances, and standard of workmanship. Build mockups using materials specified for the completed Work, and in compliance with recommendations of manufacturer.

          - Obtain [Architect’s] <Insert other Entity> approval of mockups prior to starting construction.

          - Viewed in light similar to project completion.

          - Mock-up construction performance should demonstrate actual construction methodology to the extent possible. Differences in equipment and actual methodology will cause variations and differences between mock-up and finished floor.

          - Demonstrate curing, finishing, and choice of protection of architectural concrete.

          - Maintain mockups, marked and undisturbed during construction to provide a baseline standard for assessing completed Work.

          - Remove mockup when directed.

Specifier Note Retain paragraph below and delete paragraph above if mockups may remain as a part of the Work.

          - Approved, undisturbed, and undamaged mockups may remain as a part of the Work.

        - Protection of Concrete Finishes: Provide protection for concrete slab finishes as indicated in manufacturer’s written instructions, 310R-19, and as follows:

          - Provide protection of concrete finishes from any contact with any substance that contains petroleum, acids or detergents.

            - Prohibit vehicle transit and parking on concrete surfaces without providing protection.

            - Prohibit storage, transit or use of hydraulic equipment on concrete surfaces without providing protection.

            - Prohibit construction operations that include the use of substances listed above without providing approved protection.

          - Provide protection to finished concrete surface from any materials placed and/or stored on the surface, including but not limited to:

            - Steel and iron.

            - Petroleum based products.

            - Vehicles and machinery.

            - Hydraulic fluid.

            - Paints and coatings.

            - Paper and plastic packaging.

            - Aggregates.

            - Food and beverages.

          - Surface Contaminant Cleaning Procedure:

            - Provided by system manufacturer.

            - On-site spill kits:

              - Solid removal.

              - Liquid removal.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver material in original containers with unbroken seals, bearing manufacturer labels indicating brand name and directions for storage.

        - Protect materials from weather and elements. Do not allow liquid products to freeze.

      - PROJECT CONDITIONS

        - Maintain environmental conditions on day of placement as recommended by treatment manufacturer and certified installer.

        - Changes to placement schedule for environmental conditions from certified installer recommendations shall be approved in writing by Owner’s Construction Manager prior to implementation.

        - Hot and cold weather concreting shall be in accordance with ACI 305.1 (hot weather) and ACI 306.1 (cold weather) except as otherwise specified herein.  In case of conflict, provisions stated herein shall prevail over ACI standard specifications.

        - Slab Conditions: Ff/Fl 50/35 on slab on grade and Ff/35 for slab on deck.

      - MANUFACTURER SPECIAL WARRANTY

        - Provide manufacturer’s 10-year warranty providing coverage that architectural concrete will remain water resistant, non-off-dusting, hardened and abrasion resistant throughout warranty period. Must accompany a time of installation report by certified installer, verified by manufacturer’s consultant and/or Corporate Office.

        - Must be installed by the manufacturer’s certified installer. Certified Craftsman Warranty: 1 year for installation defect.

- PRODUCTS

      - MANUFACTURERS AND PRODUCTS

        - Subject to compliance with requirements, provide products by the following:

          - Basis of Design: Green Umbrella Architectural Concrete Systems, Inc. 20 Jetview Dr. Rochester, NY 14624, basis of design manufacturer. Technical and Architectural Support:(844) 200-7336, info@greenumbrellasystems.com

          - No substitutions.

      - PERFORMANCE REQUIREMENTS

        - Abrasion Resistance:

          - ASTM C779/C779M:

            - 0.25 mm at 30 minutes and 0.53 mm at 60 minutes

          - ASTM C944/C944M:

            - 0.038 mm.

Specifier Note: Retain BS-EN Standard if project requires it.

          - BS EN 13892-4:2002

            - Special/SF.

            - Special/DF.

        - Slip Resistance: Minimum Dynamic Coefficient of Friction of 0.42, per ANSI/NFSI B101.3.

        - Water Vapor Transmission of Materials: ASTM E96/E96M of 0.34 g/h/m2.

        - Ultra-Violet Light and Water Spray: No adverse effects to ultra-violet and water spray, per ASTM G152.

      - MATERIALS

        - Concrete: Provide ready-mixed concrete from a single design mix and single batch plant for the entire Project specified herein. Provide concrete in conformance with Division 03 Section "Cast-In-Place Concrete" and ASTM C94/C94M.

          - Admixtures: Use only admixtures compatible with finish system. Do not use admixtures containing chlorides.

        - Reinforcing Fiber: FiberLite fiber reinforcement complying with ASTM C1116/C1116M.

      - CONCRETE EVAPORATION REDUCER/ FINISH AID/ CURATIVE / FIXATIVE / DENSIFIER SYSTEM

        - System Description: Clear, penetrating, reactive, VOC-compliant system consisting of combined evaporation reducer/ finish aid/curative / fixative / densifier/ sealer agents to promote proper cure and produce mechanically and chemically densified power troweled concrete surfaces.

          - Basis of Design Product: Green Umbrella, IceStart & IceStop.

- Specifier Note: Retain subparagraphs below if floor is in the dry and protection is to cover the slab during construction. Select product to match if it is outdoors or indoors.

        - Interior Slab In Dry Protection Materials:

          - Product: Green Umbrella Ramboard:

            - Forest Stewardship Council (FSC) certified. Recycled and recyclable materials.

            - Roll Dimensions (W x L): 38 inches x 100 feet (965 mm x 30.5 m). 317 sq ft. Rolls per Pallet: 16.

            - Green Umbrella Ramboard Vapor-Cure Tape: Vapor-Cure used to cover seams which prevents tape lines. Allows vapors and moisture to escape from concrete.

            - Roll Dimensions (WxL): 3 inches x108 feet (76 mm x 32.9 m) Rolls per Box: 16.

        - Cleaning Agent:

          - Product: CleanMaintain with Slip Resist:

            - Slip resistance enhancing.

            - pH neutral.

          - Product: GreenClean and Degreaser:

            - Enzyme degreaser.

            - pH neutral.

            - Water treatment friendly.

          - Product: GreenClean Spill Kit:

            - Solid spill kit.

            - Liquid spill kit.

            - 72-hour recovery.

- EXECUTION

      - EXAMINATION

        - Examine architectural concrete substrates with concrete subcontractor, for conditions that may affect the Work. Is this only for polishing. I thought we were taking this out so just focused on GreenIce. This whole section A to E. Need to review.

        - Verify preparations and placement of concrete is in accordance with ACI standards and manufacturer’s written instructions.

Specifier Note: Retain subparagraph below if Green Umbrella components are required to be added to the concrete mix at the concrete batch plant.

          - Verify coordination with concrete mix plant, use of correct dosage, and proper mixing per ASTM C94/C94M.

        - Verify ambient and surface temperatures to be in accordance with manufacturer’s requirements for all products for the work.

Specifier Note: Retain subparagraph below if "CanvasControl & Profile System" or "GreenIce Cure & Profile System System".

        - Verify concrete compressive strengths are in accordance with Contract Documents.

        - Verify that the owner’s testing agency results for Mohs Hardness test per ASTM C1895 are in accordance with this specification.

      - PREPARATION

        - Site Conditions

          - The building shell shall be completed sufficiently to keep out wind, rain, snow or other adverse weather affects that could damage the concrete work.

          - Provide suitable water, power, lighting and ventilation.

            - Provide minimum lighting of 40-foot candles (440 lux) measured at floor surface.

          - Provide and maintain minimum floor slab temperature of 50 degrees F.

        - All penetrations, drains, floor embeds, or conduit shall be cut, capped, clearly identified and made safe prior to any concrete work.

        - Prepare equipment to be used in application of finish system materials according to finish system manufacturer’s written instructions.

        - Completely clean liquid treatment application sprayers free of any potential contaminating material and make ready for application.

        - Prepare power trowels per finish system manufacturer’s written instructions, cleaned and ready to trowel with accompanying spray of finish system materials. (Recommended to keep Finish Trowel dedicated for final Combo Blade finish process.)

      - APPLICATION

        - Concrete finish system shall be incorporated into the placement of new concrete slabs according to the manufacturer's instructions. Proceed with placement of concrete under the supervision of finish system manufacturer’s representative.

        - All concrete placement and finishing is to be performed in accordance with curing/finishing system manufacturer’s written instructions.

          - Troweled Finish: Provide troweled finish as indicated herein and according to manufacturer’s written instructions.

        - Installation of Evaporation Reducer/ Finish Aid/Curative / Fixative / Densifier/ Sealer System (GreenIce IceStart): Apply in three applications as follows:

          - Apply Green Umbrella, lceStart through high-volume, low-pressure sprayers prior to the first bull float process.

            - Spray-apply at a rate recommended by the manufacturer.

            - Perform bull float process as recommended by manufacturer and referenced ACI standard.

          - Apply second application at a rate recommended by the manufacturer, either by sprayers or through sprayers on power trowels. Pan material into the surface of the concrete. Power trowel as recommended by manufacturer and ACI standard.

          - Apply third application at a rate recommended by the manufacturer, either by sprayers or through sprayers on power trowels. Pan material into the surface of the concrete. Power trowel as recommended by manufacturer and ACI standard. Perform Combo Blade finishing as recommended by manufacturer and ACI standard.

          - Be prepared to apply setting/curing catalyst immediately upon completion of finishing operations.

        - Installation of Setting/Curing Catalyst:

          - Apply Green Umbrella, IceStop using high-volume, low-pressure (pump or battery powered) sprayers at a rate recommended by manufacturer.

          - Allow setting/curing/catalyst to remain on the slab for a minimum of 30 minutes wet dwell time and allow to dry. Do not add water.

          - Verify that the treatment has completely dried, indicating that curing system installation is complete.

      - EQUIPMENT

        - Refer to manufacturer’s written instructions for requirements of installation equipment, including but not limited to sprayers, power trowels, burnishers, auto scrubbers, saws, and dust collection system.

      - FIELD QUALITY CONTROL

        - Arrange for the approved system manufacturer's technical representative to evaluate finished concrete work for compliance with the specified requirements.

        - The Owner reserves the right to engage a testing agency to verify compliance with the specified performance values for the finished work.  Cooperate with the Owner's testing agency in scheduling and conducting tests.

          - Concrete work that fails to comply with the specified performance requirements as determined by certified test results shall be replaced at no additional cost to the Owner.

      - PROTECTION AND CLEANING

        - Protect finished concrete surfaces for the remainder of the construction period as recommended by the manufacturer.

        - Prohibit wheeled traffic on finished surfaces for time period recommended by the Green Umbrella Craftsman.

        - Protect finished floor as specified above and as indicated in manufacturer’s written instructions and 310R-19.

        - Thoroughly sweep floor. Auto scrub with manufacturer’s cleaning agent, neutral pH CleanMaintain w/SlipResist or DeepClean & Maintain.

        - Provide daily scrubbing of the entire exposed concrete slab surface with riding equipment that utilizes only pads and water, Daily scrubbing shall continue from time of dried initial application of surface densifier until time of turnover.  Use white or red pads, cleaned or replaced daily, and avoid using excessive downward head pressure that may damage the slab surface

END OF SECTION 033509